# PEBA-LW                  Technical Data Sheet

PEBA-LW is a thermoplastic elastomer based on PEBA90A (hardness 90A), utilising a more environmentally friendly physical foaming / 3D printing synchronous foaming process. Its core structure comprises a "PEBA molecular chain elastic skeleton + closed-cell foamed microstructure", retaining PEBA's inherent high toughness, high resilience, wear resistance, and wide temperature adaptability while achieving 100%-200% weight reduction through foaming.Furthermore, by adjusting foaming parameters, it flexibly adapts between "high-foaming lightweight" and "low-foaming high-resilience" configurations. This multifunctional thermoplastic elastomer material balances "weight reduction requirements" with "elastic performance", making it widely applicable in scenarios with differentiated demands for weight, resilience, and cushioning.

Basic Information

| Characteristics | • Exceptional toughness • Superior resilience • Adjustable density | • hardness adjustability • Lightweight • Wide temperature adaptability |
| --- | --- | --- |
| Applications | • Custom footwear materials • Sports equipment • Lightweight fixtures | • Industrial components • Cushioned packaging • Wearable accessories |
| Manufacturing Processes | • 3D printing | • FDM printing |

Basic physical properties              Test methods             Data

| Density | GB/T 1033 | <1.24 g/cm³ |
| --- | --- | --- |
| Melt Index (190°C, 2.16 kg) | GB/T 3682 | 5–15 g/10 min |
| Tensile strength | GB/T 1040 | 14 MPa |
| Elongation at break | GB/T 1040 | 500 % |
| DIN abrasion | ISO 4649 | <50 mm3 |

Printing performance                 Test method              Data

| Tensile strength (Z-axis) | GB/T 1040 | 5.5 MPa |
| --- | --- | --- |
| Elongation at break (Z-axis) | GB/T 1040 | 30 % |
| Tensile strength (XY axis) | GB/T 1040 | 14MPa |
| Elongation at break (XY axes) | GB/T 1040 | 500% |
| Notched Charpy impact strength (XY axis) | GB/T 1843 | NB |

| Maximum rebound | ASTM D2632 | 60% |
| --- | --- | --- |
| Maximum volumetric flow rate | Rotating Vase | 6.5 mm3/s |
|  |  | Note: All printing performance tests were conducted under non-foaming conditions. |

Chemical Properties                            Data

| High chemical stability; foaming modification does not alter the chemical nature of PEBA, only forming a closed-cell microstructure through physical foaming. Chemical properties are based on the PEBA matrix, while also incorporating the inert characteristics of foamed microspheres. |  |
| --- | --- |

Recommended printing parameters          Data

| Drying Conditions | 70°C, 6–8 hours |
| --- | --- |
| Nozzle Temperature | 210–270 °C |
| Nozzle Size | 0.4 mm |
| Baseplate material | PEI |
| Bed temperature | 35–75°C |
| Fan size | 100% |
| Printing speed | 20–70 mm/s |

Printing Precautions

- It is recommended to re-dry the filament upon receipt. After the filament has been exposed to air for a period following unpacking, re-drying is advised to enhance printing results.

- It is recommended to use a brand-new hotend. Do not use a hotend that has previously printed fibre-reinforced filament to print PEBA-LW.

- Ensure the extruder is free of foreign objects and that the feed gears show no signs of wear, as these issues may cause material slippage and prevent consistent, uniform extrusion.

- Printing flexible filament requires low-resistance, smooth feeding. Excessive feeding resistance may cause insufficient extrusion. We recommend using a spool dryer with bearings or installing a low-resistance spool holder with bearings.

Mechanical Properties Test Conditions

| Tensile test specimens GB/T 1040 | Bending test specimens GB/T 9341 | Impact test specimen GB/T 1843 |
| --- | --- | --- |

Wire performance is tested using eSUN's standard printed samples for design reference purposes. Actual printability may be influenced by various factors including printer type, print parameters, and printing environment.

| Printing Test Conditions |  |
| --- | --- |
| Nozzle Temperature | 210–270 °C |
| Bed Temperature | 35–75 °C |
| Number of outer layers | 2floor |
| Number of top/bottom layers | 3floor |
| Internal filling | 100% |
| Fan speed | 100% |
| Maximum Volume Flow | 50 mm/s |

*Based on testing with Bambu P1S 0.4 mm nozzle and Orcaslicer 2.1.0.

Note

Information regarding this product provided by eSUN or on behalf of eSUN, whether in the form of data, recommendations, or otherwise, has been thoroughly researched and is believed to be reliable in good faith. However, please note that the product is sold "as is". eSUN assumes no liability and makes no representations or warranties, express or implied, regarding the merchantability, fitness for a particular purpose, or any other nature of the information or product. This disclaimer does not exempt the seller from any applicable terms of sale.